PRODUCT  DATA  SHEET

PRODUCT  DATA  SHEET

###### SL NT HT Series

SYNTHETIC NON-TOXIC HIGH TEMPERATURE GREASE

###### SL NT HT Series

SYNTHETIC NON-TOXIC HIGH TEMPERATURE GREASE

G

PRODUCT  DESCRIPTION

PRODUCT  DESCRIPTION

SL-NT-HT is part of a second generation of high performance synthetic lubricants specially designed to meet the requirements of the food, cosmetic and pharmaceutical industries.  The growing trend to extend intervals between lubrication imposes stringent demands on grease performance service.  Temperature extremes, shock loadings, vibration and water washout conditions add to these demands.

SL-NT-HT is heavy duty synthetically thickened grease which employs a highly thermal stable synthetic base fluid.  It will not wash out, pound out or melt and run out under severe conditions.

TYPICAL  CHARACTERISTICS

TYPICAL  CHARACTERISTICS

SL-NT-HT is non-toxic, water white, tasteless, odorless grease that complies with FDA regulation Title 21, CFR 178.3570 and NSF H-1 rating. It is made with materials acceptable to NSF for use with food handling and food processing equipment.

SL-NT-HT is a non-toxic extreme high temperature grease recommended for applications where grease lubrication is called for and where continuous temperature exceeds 260°C (500°F).  Maximum working temperature for SL-NT-HT  should be considered to be approximately 425°C (800°F), however, higher temperature on an intermittent basis are acceptable to the 540°C (1000°F) point.

NLGI Grade		0	  1                                2			ASTM D-1092

Worked Penetration	                       355-385                  310-340                     265-295			ASTM D-  217

Dropping Point	                      ------------------------  None  ------------------------------      		ASTM D-2265

Oxidation Stability 	                      ------------------------- 2 -----------------------------------      		ASTM D-  942

Psi Drop @ 100 hrs

Rust Preventative	                      -------------------------	 1a  --------------------------------     		ASTM D-1743

Water Washout	                      -------------------------	1.1  --------------------------------    		ASTM D-1264

Extreme Pressure	                      ----------------------- 25+ (55)  ----------------------------			ASTM D-2509

Timken OK Load Kg (Lb)

Four Ball Wear	                      ------------------------ 0.7mm ------------------------------			ASTM D-2266

Food Grade Status	                      -------------------------   H1   -------------------------------			     NSF

NSF Registration	                        133572                   133573                      133574

Appearance 	                      --------------------  Clear, Smooth  ------------------------

PIN #                                                 06561                    06562                         06563

TO ORDER or FOR ADDITIONAL INFORMATION

TO ORDER or FOR ADDITIONAL INFORMATION