PRODUCT  DATA  SHEET

G

- SCO HFC

- Series

REFRIGERANT COMPRESSOR

PRODUCT  DESCRIPTION

| SCO HFC SERIES are synthetic polyol ester (POE) based lubricants for refrigerant compressors. SCO HFC SERIES are blended from high purity polyol esters having excellent miscibility and compatibility with new generation HFC refrigerants and lubricity. A special additive package enhances wear protection for both steel-on-steel and steel-on-aluminum surfaces. They are chemically and thermally stable so that systems stay cleaner even under severe operating conditions. | Although this Series is recommended for automotive systems, they also meet the lubrication requirements of a broad spectrum of industrial applications employing positive displacement and dynamic compressors. They can also be used with chlorinated refrigerants such as CFC-12, HCFC-22 and R-502. |
| --- | --- |

PRODUCT  ADVANTAGES

• Low Pour Point

• Improved Compressor Efficiency

• Improved Wear Protection

• Extends Service Life

• Extends Drain Intervals

• Chemically Stable

• Eliminates Sludge Formation

TO ORDER or FOR ADDITIONAL INFORMATION

PRODUCT  DATA  SHEET

- SCO HFC

- Series

REFRIGERANT COMPRESSOR

TYPICAL  CHARACTERISTICS

|  | HFC 32 | HFC 46 | HFC 68 | HFC 100 | HFC 150 | HFC 220 |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| ISO Viscosity Grade | 32 | 46 | 68 | 100 | 150 | 220 | ASTM D-2422 |
| Viscosity cSt @100°C @ 40°C | 6.4 31.3 | 9.5 46 | 11.1 65 | 13.5 97 | 15.1 170 | 30.9 217 | ASTM D- 455 |
| Viscosity Index | 102 | 113 | 104 | 98 | 99 | 185 | ASTM D-2270 |
| Flash Point °C (°F) | 500°C(260°F) | 572°C(293°F) | 575°C(300°F) | 578°C(301°F) |  | 590°C(310°F) | ASTM D- 92 |
| Pour Point °C (°F) | -58°C(50°F) | -56°C(-49°F) | -54°C(-48°F) | -49°C(-45°F) |  | -32°C(-25°F) | ASTM D- 97 |
| Copper Corrosion |  |  |  |  |  |  |  |
| Thermal Stability |  |  | NO | CHANGE |  |  | ASHRAE 97-1983 |
| Four Ball Wear Test Wear Scar (mm) | 0.93 | 0.80 | 0.80 | 0.90 | 0.86 | 0.79 | ASTM D-2783 |
| Specific Gravity, 15.6°C (60°F) |  |  |  |  |  |  |  |
| PIN # | 14332 | 14346 | 14368 | 14390 | 14395 | 14399 |  |

TO ORDER or FOR ADDITIONAL INFORMATION