PRODUCT  DATA  SHEET

###### SL-WR

###### WHITE #2

WATERPROOF GREASE

PRODUCT  DESCRIPTION

SL-WR White is an outstanding synthetic grease for every phase of lubrication (including, but not limited to) in the presence of water, steam, most acids or salts.  There is little or no washout, breakdown, or emulsification when subject to temperatures under 205°C (400°F).  SL-WR White showed superior cohesiveness and tenacity after being “worked” for 72 hours.  In cold temperature tests at 17.8°C (0°F), it showed superior film coating and excellent pumpability.

SL-WR White is formulated with materials acceptable to FDA and NSF for use with food handling and food processing equipment.  SL-WR White is unaffected by most food products.  It shrugs off beer, alcohol, beverages, salt, starches, jellies, sugar and flour.

TYPICAL  CHARACTERISTICS

Even the cleaning chemicals used in food plants have

little effect on its lubricating properties.  It is recommended for all slides, cams, bearings and all types of mechanical equipment especially those subject to water conditions and/or high temperature.  Because of the foregoing and its white color, SL-WR White is highly recommended for food plants, dairies, meat packing houses, bakeries, pharmaceutical plants, hospitals, textile plants, etc.

It is also available in NLGI grades 0 and 1.

NLGI Grade         	2 					ASTM D-1092

Worked Penetration	265-295					ASTM D-  217

Dropping Point	None  					ASTM D-2265

Oxidation Stability

Psi drop @ 100 hrs	-1					ASTM D-  942

Rust Preventative	1a					ASTM D-1743

No Stain

Water Washout	.5					ASTM D-1264

Extreme Pressure	34+ (75)					ASTM D-2509

Timken OK Load Kg (Lb)

Four Ball Wear	.6 mm					ASTM D-2266

Solids	Zinc Oxide

Food Grade Status	H1					NSF

NSF Registration	133570

Appearance	White Opaque

PIN #		                                                            03109

TO ORDER or FOR ADDITIONAL INFORMATION