PRODUCT  DATA  SHEET

###### SRC #1 “S”

SYNTHETIC ROLLER CHAIN

PRODUCT  DESCRIPTION

SRC #1 Roller Chain “S” is a metallic roller chain lubricant with a high percentage of homogenized submicron particles self-lubricating metallic solids.

The carrier will act as a medium to carry the solids and deposit them into all internal working areas of the chains to guarantee maximum reduction of friction and subsequently elimination of wear.

The non-oily carrier will assure maximum cleanliness providing adequate corrosion protection and water displacement while acting as a rust and corrosion preventative.

TYPICAL  CHARACTERISTICS

DIRECTIONS:  Shake can well before use.  Can temperature should be 18˚C (65˚F) or warmer.  (WARNING: Never use direct heat to warm aerosol cans!  ONLY warm water should be used!) Spray part to be lubricated, repeating as necessary.

Sentinel’s “S” line of spray lubricants is a non-ozone depleting product specially formulated for industry.

Sentinel’s “S” line contains no CFC’s, HCFC’s, Methyl chloroform, or any other material known to affect the stratospheric ozone.

Viscosity cSt	@ 100˚C	3.6

@   40˚C	13.7					         ASTM D-  445

Viscosity Index	144					         ASTM D-2270

Pour Point ˚C (˚F)	-48  (-50˚F)					         ASTM D-    97

Flash Point ˚C (˚F)	120 (248˚F)					         ASTM D-    92

Fire Point ˚C (˚F)	133 (271˚F)					         ASTM D-    92

Foam Sequence I, II, III	Nil					         ASTM D-  892

Demulsibility, 82˚C	Pass					         ASTM D-1401

Copper Corrosion, 121˚C (250˚F)

3 Hours	1a					         ASTM D-  130

Rust Test	Pass					  ASTM D-665 A&B

Solids	Molybdenum Disulfide

Appearance	Light Gray

USDA Classification	H-2

Net Weight per 20oz Aerosol Can	15 oz. (425g)

PIN #							         01019

TO ORDER or FOR ADDITIONAL INFORMATION