PRODUCT  DATA  SHEET

G

###### SL-OG

OPEN GEAR COMPOUND

PRODUCT  DESCRIPTION

Sentinel SL-OG is a unique synthetic metallic compound designed for general purpose open gear lubrication.  It has a high tack content that prevents it from slinging out even at high RPM’s.  It is specifically formulated to stay on exposed and open gears, resisting extreme temperatures as well as extreme pressures from close moving parts.  SL-OG has a thermal range from -28°C (-20°F) to 232°C (450°F) and an E.P. rating in excess of 150,000 psi.

Sentinel SL-OG has metallic particles incorporated into its synthetic carrier, making it bronze in color and giving it greater plating action.

TYPICAL  CHARACTERISTICS

Under pressure, these solid lubricants are carried into the gear faces and moving surfaces, all score marks, pits and grooves or other facial imperfections are filled in and a uniform low friction coating forms.  Shock and noise are reduced, uneven wear is prevented and it can even be applied while equipment is running.

Unlike petroleum based open gear lubes, SL-OG is not susceptible to water and is not affected by heat, cold, or extreme pressures.  It will not harden in cold weather, or melt out in warm weather.

NLGI Grade         	1					ASTM D-1092

Worked Penetration	310-340					ASTM D-  217

Dropping Point	None  					ASTM D-2265

Oxidation Stability

Psi drop @ 100 hrs	-1					ASTM D-  942

Rust Preventative	1a					ASTM D-1743

No Stain

Water Washout	0.6					ASTM D-1264

Extreme Pressure	45+ (100)					ASTM D-2509

Timken OK Load Kg (Lb)

Four Ball Wear	.6 mm					ASTM D-2266

Solids	Copper Bronze

USDA Rating	H-2

Appearance	Gold Metallic Tacky

PIN #		                                                            03057

TO ORDER or FOR ADDITIONAL INFORMATION