PRODUCT  DATA  SHEET

G

###### SCO REF Series

###### REFRIGERATION OIL

PRODUCT DESCRIPTION

Sentinel’s SCO-REF Oil Series are a family of fully synthetic industrial lubricants developed specifically for refrigeration compressors.  They are especially formulated synthesized hydrocarbon lubricants for severe service under conditions that are beyond the capabilities of conventional mineral oils.  In addition, they improve the performance and efficiency of standard refrigeration systems compared to conventional mineral oils.

Sentinel SCO-REF have very low pour points, zero wax content, a high natural viscosity index and high thermal stability.  They exhibit greater chemical stability in the presence of refrigerants and other system components, and have a low volatility.  Their low solubility makes them suitable for systems using refrigerants such as R12, R22, R114 and ammonia.

TYPICAL CHARACTERISTICS

Improved wear protection at high temperatures

No deposit formation in low temperature systems

Fewer discharge valve deposits

Improved compressor efficiency

TO ORDER or FOR ADDITIONAL INFORMATION

###### SCO REF Series

###### REFRIGERATION OIL

TYPICAL  CHARACTERISTICS

SCO-REF 32       SCO-REF 46        SCO-REF 68         SCO-REF 100	  SCO-REF 150	      SCO-REF 220      	ASTM METHOD

ISO Viscosity Grade		       32						   46	         68		            100				           150			       220		D-2422

SAE Viscosity Grade 			       10  				    10W20	         20	    	30				            40			        50

Viscosity cSt @ 100°C	          5					       7.9	         10		   	14					            20			          25			D-445

@   40°C		         29					      43.9	         62	    	99					           160	          220			D-445

Viscosity Index			      132				        145	         148		   	144					            145		           143			D-2270

Pour Point °C (°F)	  		-54(-65)			     -50(-58)	     -48(-55)		        -43(-45)				          -40(-40)			     -40(-40)			D-97

Flash Point °C (°F)			  218(425)			   218(425)	     222(431)		        229(445)				          248(478)		     250(482)			D-92

Foam Sequence I, II, III					------------------------------------------------------------------  Nil  ---------------------------------------------------------------				D-892

Demulsibility,	-------------------------------------------------------------   40/40/0(15)   --------------------------------------------------------				D-1401

54.4°C (130°F)

Four Ball Wear, mm 40kg,			------------------------------------------------------------------  0.5  ---------------------------------------------------------------     				D-2266

1200 rpm, 75°C (1hr)

Copper Corrosion 			------------------------------------------------------------------  1a   ---------------------------------------------------------------			D-130

121C(250F), 3 hrs

Rust Test                                -----------------------------------------------------------------  Pass  --------------------------------------------------------------			D-665A&B

Color Observed                      ---------------------------------------------------------------    Clear  -------------------------------------------------------------

Food Grade Status	        ------------------------------------------------------------------  H1  --------------------------------------------------------------	        NSF

NSF Registration	          137650                  137651                   137652                      137653                     137654                       --------

PIN#	       11301	    		       11310	   		       11305		           11307    			           11312			11315