PRODUCT  DATA  SHEET

G

###### TURBINE OIL SERIES

PRODUCT  DESCRIPTION

Sentinel’s line of synthetic Turbine Oils is fully formulated to meet the desirable properties of low volatility and good viscosity/temperature characteristics and stability requirements of steam, gas, hydroelectric and marine gear turbine installation.

The specially selected additive systems give these products outstanding resistance to oxidation and corrosion of metal surfaces.  All grades are carefully balance with rust and oxidation inhibitor package and an effective anti-foamant, which provides excellent anti-foam and air release characteristics.

PRODUCT  ADVANTAGES

Meets and surpass the following Specifications:

General Electric GEK-32568E

GEK-28143A

GEK-46506D

GEK-27070

Sulair Turbines ES 9-224

Cincinnati Milacron P-38, P45-P54, P55, P62

Alstom Power HTGD 90117

Siemens Westinghouse M-Spec 55125Z3

Siemens TLV 901304

ABB ALSTOM

General Motors L52 Specification LJ

Denison HF1

DIN 51524, Part 1

MIL-H 17672 D

Outstanding Oxidation Stability

Excellent Water Separation

High Viscosity Index

Improved Efficiencies

Extended Drain Interval

Reduced Oil Consumption

Reduced Maintenance Cost

Improved Safety Excellent High Temperature Stability

TO ORDER or FOR ADDITIONAL INFORMATION

TURBINE OIL SERIES

TYPICAL  CHARACTERISTICS

32				46	  			68	 100  					  150				ASTM METHOD

ISO Viscosity Grade	     	32	 	46	  			68		 100			150					D-   2422

SAE Viscosity Grade		10		20W	20		     30	                             40        				   SAE J-    300

Viscosity cSt  @ 100C	     	5.9		7.9		10.3		   14.3		    20							D-     445

@   40C	  		31.5	43.9		          67			  101			  160 				D-     445

Viscosity Index	 		135	145		         146               	  131                 	         142                 			D-   2270

Pour Point C (F)                 	 -48(-55)       	-46(-50)	  	 -43(-45)          -40(-40)		    -37(-35) 		         D-       97

Flash Point C (F)                	231(448)      	233(451)                  236(457)         249(480)          	           250(482)      					D-       92

Foam Sequence I, II, III                                   -----------------------------------------------------Pass-------------------------------------------------						D-     892

Demulsibility 82C                                          -------------------------------------------------40/40/0(15)--------------------------------------------        					D-   1401

Four Ball Wear, mm 40kg, 1200 rpm,             ------------------------------------------------------0.4-------------------------------------------------		D-   2266

75°C (167˚F) 1hr

Copper Corrosion 121C(250F), 3 hrs            ----------------------------------------------------1a----------------------------------------------------          			D-     130

Oxidation Life, Hours	      -------------------------------------------------16, 000+-----------------------------------------------			D-     943

Rust Test                                                           ----------------------------------------------------Pass--------------------------------------------------            				D-665AB

TAN                                                                  ------------------------------------------------------.05-------------------------------------------------		 		D-    664

Conradson Carbon Residue, %                        ---------------------------------------------------<0.02-------------------------------------------------				D-    189

PIN#			        11250          		11253              	11255             11257		11260