PRODUCT  DATA  SHEET

G

###### ST-WR Series

WIRE ROPE LUBRICANTS

PRODUCT  DESCRIPTION

\

Sentinel® ST wire rope lubricants are compounded with .02 micron particles of Teflon®* which provide exceptionally low frictional qualities with positive anti-wear protection.  They are formulated to prolong the life of wire rope, support cables and sheaves.  These lubricants have extreme pressure properties superior to heavy-duty gear oils and greases.  They have very low surface tension and polar properties, allowing for maximum penetration to the core of even the largest rope.  In this way the lubrication is performed from the innermost core out, thereby assuring complete lubrication of each individual strand.  This provides full protection against corrosion wear.

The high water displacing qualities provide a positive monomolecular film on all rope surfaces, which act as a release agent reducing dirt and dust build up and permitting easy inspection of the rope.

Sentinel® Wire Rope lubricants can be applied by brushing, dipping or spraying.  Sentinel Wire Rope Lubricants are satisfactory for automatic lubricating systems because they remain fluid -40˚C (-40˚F).

* Registered trademark of E.I. Dupont

TYPICAL  CHARACTERISTICS

ST-WR 1 	 ST-WR 2  	ST-WR XL

ISO Viscosity Grade                       150	                      680		         	          ---		          ASTM D-2422

Viscosity cSt @ 100˚C                   16.3	                      41		                        1.7	          ASTM D-  445

@   40˚C               139	                     680                                        5.0

Viscosity Index                              123	                     100		                       126	          ASTM D-2270

Pour Point ˚C (˚F)                          -40 (-40)	                   -18 (0)		      -48(-55)	          ASTM D-    97

Flash Point ˚C (˚F)                        235 (455)	                   243 (470)		      190 (374)	          ASTM D-    92

Demulsibility, 82˚C                      ---------------------------40/40/0 (30)-----------------------------------            ASTM D-1401

Four Ball Wear, mm

40 kg, 1200 rpm, 75˚C (1 hr)  ----------------------------40----------------------------------------------	          ASTM D-2266

Rust Test                                        ---------------------------Pass-------------------------------------------	          ASTM D 665 A&B

Appearance on Wire Rope     Light Lubricating Film       Heavy Film                 Light Lubricating Film

Appearance	                       Green	                   Dark Grey                              Dark Amber

PIN #                                          08133		       08137                                       08130

TO ORDER or FOR ADDITIONAL INFORMATION