PRODUCT  DATA  SHEET

G

###### SL-M2 “S”

MULTI-USE EXTREME

PRESSURE GREASE

PRODUCT  DESCRIPTION

SL M-2 “S” is a new synthetic formulated with molybdenum disulfide to obtain the optimum in anti-wear and extreme pressure qualities.  It is practically neutral in pH and is extremely water-resistant.  Therefore, it is not affected by water (hot or cold), steam or most acids and salts.

When heavy bearing loads are encountered by SL M-2 “S” and boundary lubrication occurs, molybdenum disulfide is activated to form a continuous monomolecular film.  This film on metal surfaces resists metal to metal contact and reduces wear in “contact lubrication.”

SL M-2 “S” also will lubricate better under hydrodynamic lubrication conditions because of the exceptional mechanical stability of this grease.  Additionally, its high drop point makes SL M-2 “S” a far superior multi-use grease.

DIRECTIONS:  Shake can well before use.  Can temperature should be 18˚C (65˚F) or warmer.  WARNING:  Never use direct heat to warm aerosol cans!  Only warm water should be used!)  Insert plastic extender tube for pin point application.  Apply liberally to area to be lubricated.  Wipe off excess.

Sentinel’s “S” line of spray lubricants are non-ozone depleting products specially formulated for industry.

Sentinel’s “S” line contains no CFC’s, HCFC’s, Methyl chloroform, or any other material known to affect the stratospheric ozone.

TYPICAL  CHARACTERISTICS

NLGI Grade	2					        ASTM D-1092

Worked Penetration	265-295					        ASTM D-  217

Dropping Point	None					        ASTM D-2265

Oxidation Stability	-1					        ASTM D-  942

Psi Drop @ 100 hrs

Rust Preventative, No Stain	1a					        ASTM D-1743

Water Washout	.9 					        ASTM D-1264

Extreme Pressure	34+ (80) 					        ASTM D-2509

Timken OK Load Kg (Lb)

Four Ball Wear	.4mm					        ASTM D-2266

Solids	MoS2

Appearance	Dark Metallic

USDA Classification	H-2

Net Weight per 20oz Aerosol Can	15 oz. (425g)

PIN #							       01028

TO ORDER or FOR ADDITIONAL INFORMATION