PRODUCT  DATA  SHEET

G

###### SL-PTFE

POLY TETRA

FLUORO ETHYLENE

(PTFE) GREASE

PRODUCT  DESCRIPTION

Sentinel SL-PTFE is a multi-purpose synthetic base grease formulated with micronized Polytetrafluoroethylene (PTFE) powder designed for applications requiring slip and heat stability.  The unique properties of SL-PTFE provide distinct advantages over other lubricating solids and insure extended protection on the surfaces.

The micron-size particles of PTFE fill voids on the surfaces lubricated forming a barrier layer, and thus reduce friction between mating surfaces insuring extended protection on the surfaces.

TYPICAL CHARACTERISTICS

SL-PTFE contains no soaps, salts, or metal based gellants.  It remains pliable, will not harden or crack, and resists changes due to mechanical work.

SL-PTFE demonstrates exceptionally good load-carrying capabilities and long-life protection against corrosion, rust, friction, and wear.

NLGI Grade	2					        ASTM D-1092

Worked Penetration	265-295					        ASTM D- 217

Dropping Point	None					        ASTM D-2265

Oxidation Stability	-1					        ASTM D- 942

Psi Drop @ 100 hrs

Rust Preventative	1a					        ASTM D-1743

No Stain

Water Washout	.9 					        ASTM D-1264

Extreme Pressure	36+ (80)					        ASTM D-2509

Timken OK Load Kg (Lb)

Four Ball Wear	.5mm					        ASTM D-2266

Solids	PTFE

Food Grade Status	H1						NSF

NSF Registration	138838

Appearance Visual	White Smooth

PIN #		                                                            03395

TO ORDER or FOR ADDITIONAL INFORMATION