PRODUCT  DATA  SHEET

G

###### TENTER

###### FRAME OIL

PRODUCT  DESCRIPTION

Sentinel’s Tenter Frame Oil blended synthetic lubricant is capable of lubricating at high temperatures without depositing any residue, such as carbon, varnish or sludge.  Tenter Frame Oil is compounded with a blend of specifically engineered lubricating solids for added protection against wear.

Sentinel’s Tenter Frame Oil is a new base oil which was designed specifically for tenter frame applications over a wide temperature range.  Recommended for use where low corrosion of both ferrous and non-ferrous metals at high temperatures is considered to be of primary importance.

TYPICAL  CHARACTERISTICS

Sentinel’s Tenter Frame Oil applications include lithographing ovens, plywood drying ovens, tenter frames in textile mills, lens and glass forming equipment in glass plants, annealing furnaces, paint and ceramic curing ovens, and others where chains and bearings are operating at high temperatures.

Tenter Frame Oil can be applied to chains with a drip oiler, brushes or wheel, by emerging in a bath, or by spray.

Tenter Frame Oil XND is for applications where oil dripping is not acceptable or where superior retention of the oil is desired.

ISO Viscosity Grade	           			100					ASTM D-2422

Viscosity cSt @ 100˚C        				14.5 					ASTM D-  445

@  40˚C				116

Viscosity Index				127				ASTM D-2270

Pour Point ˚C (˚F)   	       		-30 (-22)			ASTM D-    97

Flash Point ˚C (˚F)             				263 (505)                    	ASTM D-    92

Fire Point ˚C (˚F) 	      				290 (554)				ASTM D-    92

Foam Sequence I, II, III				Pass					ASTM D-  892

Demulsibility, 82˚C					40 / 40 / 0 (15)			ASTM D-1401

Four Ball Wear, mm

40kg, 1200 rpm, 1 hr., 75˚C  		.43				ASTM D-2266

Copper Corrosion, 121˚C  (250˚F) 3 hrs	1a			ASTM D-  130

Rust Test			Pass				ASTMD-665A&B

USDA Classification             		H-2

PIN #	          		16110

TO ORDER or FOR ADDITIONAL INFORMATION