PRODUCT  DATA  SHEET

G

###### S-WAY OIL

###### Series

SYNTHETIC WAY OIL

PRODUCT  DESCRIPTION

Sentinel® line of Way Oils are blended from high quality, synthetically treated base oils, a superior combination of extreme pressure, anti-wear, rust and oxidation inhibitors.  In addition these oils are fortified with oiliness and special stringiness additives to impart tackiness and adhesiveness.

Sentinel® Way Oils adheres strongly to sliding metal surfaces and provide a tenacious lubricant.  The tackiness combined with exceptional lubricity offers ideal lubrication for vertical as well as horizontal ways.

The low coefficient of friction overcomes the stick-slip motion associated with slow moving machine parts even after standing overnight.  They are highly effective in controlling wear and protecting against galling.

Typical applications include sliding ways of machines including lathes, planers, shapers, drilling and tapping machines, grinders, boring machines, jig borers, milling machines and other applications requiring an adhesive, non-drip characteristic lubricant, such as enclosed gears and all types of industrial plain and anti-friction bearings.

Application methods are an oil can, oil cup, reservoir, splash, or by automatic dispensing equipment.

TO ORDER or FOR ADDITIONAL INFORMATION

###### S-WAY OIL

###### Series

SYNTHETIC WAY OIL

TYPICAL  CHARACTERISTICS

10				    20	  			30		      40					    50				ASTM METHOD

ISO Viscosity Grade	     	    32		    68		 100					150		     220					D-2422

AGMA Lubricant Number		    ---		   2EP		 3EP					4EP		     5EP

Viscosity cSt @ 100C		     6		    10		  14		 18		 23					D-88

@   40C	  		    32	    68		       100			       150			220		D-88

Viscosity Index		               136	       131                          142	                    133                           129	                        D-2270

Pour Point C (F)                 	-40 (-40)		-30 (-35)			-35 (-30)	    -32 (-25)	  -29 (-20)	  D-97

Flash Point C (F)		200 (390)	205(400)	   220 (428)		224 (435)			    230 (446)	D-92

Foam Sequence I, II, III                                   -----------------------------------------------------NIL-------------------------------------------------	  D-892

Demulsibility, 54C (130˚F)                            -------------------------------------------------40/40/0(30) --------------------------------------------            	  D-1401

Four Ball Test Wear, mm 40 kg, 1200 rpm

75˚C (1 hr)	 ---------------------------------------------------.5mm--------------------------------------------------	  D-2266

Copper Corrosion 121C(250F), 3 hrs            ----------------------------------------------------1a----------------------------------------------------            	         D-130

Rust Test                                                           ----------------------------------------------------Pass--------------------------------------------------            	         D-665AB

Timken OK Load kg/ (lb)	 36+ (80)	36+ (80)		  36+ (80)	  45+ (100)	  45+ (100)	  D-2509

Conradson Carbon                                           0.05	    0.05		  0.05		     0.06		          0.08       	         	         D-189

Appearance				      ----------------------------------------------Light Green------------------------------------------------		         D-1500

PIN#			      12250          	           12253              	12255                      12257		        12260

TO ORDER or FOR ADDITIONAL INFORMATION