PRODUCT  DATA  SHEET

###### MOLY DRY

###### FILM “S”

MOLY DRY FILM

PRODUCT  DESCRIPTION

Sentinel’s Moly Dry Film “S” provides a thin, quick dry coating of molybdenum disulfide, which is held on the surface with a blend of organic and inorganic binders.  When applied to clean metal, all metal pores, “valleys”, scratches and other microscopic recesses in the surface are filled.  After surfaces are loaded, the moly takes on a compacted nature in the recesses and serves to greatly reduce friction under loading conditions. It contains no oil, grease or graphite.

Excellent as a pre-lubrication coating on high temperature mechanisms, as an assembly lubricant, as a press fit tube, and many other high pressure point uses.

Use on casting molds, oven hardware, cans, followers, rollers, chains, cables, open gears, threaded fasteners, slides,

TYPICAL  CHARACTERISTICS

latches, locks, pins, bearings, press fits, as a break-in lube on bearings, and for many other applications.

DIRECTIONS:  Shake can well before use.  Can temperature should be 18ºC (65ºF) or warmer.  (WARNING: Never use direct heat to warm aerosol cans! ONLY warm water should be used!)  Clean mating surfaces before application, and spray area to be lubricated.  Permit to dry for a few minutes before use.

Sentinel’s “S” line of spray lubricants are non-ozone depleting products specially formulated for industry.

Sentinel’s “S” line contains no CFC’s, HCFC’s, Methyl chloroform, or any other material known to affect the stratospheric ozone.

Appearance						               Dark Gray

Lubrication, load capacity, psi						                  140, 000

Minimum Functional limits

Air Exposure, ºC (ºF)						              -120 (-250)

Maximum Functional Limits

Oxygen Free Environment, ºC (ºF)						            1090 (2000)

Air Exposure, ºC (ºF)						                398 (750)

Residue from Binder @ High Temperatures						                Soft Dust

Particle Size		                                                   Dispersion Grade

Coefficient of Friction						              0.03 – 0.06

USDA Classification						                          H-2

Net Volume per 20oz Aerosol Can						            13oz. (369g)

PIN #						                      01007

TO ORDER or FOR ADDITIONAL INFORMATION