PRODUCT  DATA  SHEET

G

###### S NT HO 20

NON-TOXIC

HYDRAULIC OIL

PRODUCT  DESCRIPTION

S-NT-HO 20 is a special non-toxic, anti-wear, anti-leak, highly refined, water white blend of U.S.P. fluids treated with synthetic compounds to produce a stable high film strength hydraulic fluid surpassing the highest purity standards.

S-NT-HO 20 offers superior protection against corrosion, rubber swelling and foaming and exhibits excellent water demulsibility characteristics.  S-NT-HO 20 contains a new non-toxic tackiness additive to arrest leakage to an absolute minimum.

TYPICAL  CHARACTERISTICS

S-NT-HO 20 meets all the FDA requirements for qualification as a white mineral oil (FDA Regulation 21 CFR 172.878) and means that the fluid maybe used in lubricants for incidental contact with food as specified in 21 CFR 178.3570.  This regulation qualifies a lubricant as a candidate for NSF rating H-1 for incidental food contact in meat and poultry plants.  The additives used in formulating S-NT-HO 20 also meet all the requirements under Regulation 21 CFR 178.3570.

ISO Viscosity Grade	68					ASTM D-2422

SAE Viscosity Grade	20					SAE J-300

Viscosity cSt @ 100˚C	10					ASTM D-  445

@   40˚C	68

Viscosity Index        	131					ASTM D-2270

Pour Point ˚C (˚F)	-37 (-35)					ASTM D-    97

Flash Point ˚C (˚F)	240 (460)					ASTM D-    92

Fire Point ˚C (˚F)	250 (480)					ASTM D-    92

Foam Sequence I, II, III	Nil					ASTM D-  892

Demulsibility 54.4˚C (130˚F)	40/40/0 (15)					ASTM D-1401

Copper Corrosion

121˚C (250˚F), 3 hrs.	1a					ASTM D-  130

Rust Test	Pass					ASTM D-  665A&B

Food Grade Status	H1					NSF

NSF Registration	138857

Appearance    	Clear, Tacky

PIN #						10515

TO ORDER or FOR ADDITIONAL INFORMATION