PRODUCT DATA SHEET

G

S-NT-GO Series

FOOD GRADE GEAR OIL

PRODUCT  DESCRIPTION

Sentinel’s Non-Toxic Gear Oil Series are specially compounded non-toxic, water white, tasteless, odorless, blend of USP fluid treated with synthetic compounds to produce a multi-purpose gear lubricant formulated to provide superior film strength and extreme pressure properties.  They are anti-wear, anti-leak, anti-foam gear oils.  They can be used in all types of enclosed gear mechanisms.

Non-Toxic Gear Oil Series is fortified with a special food grade polymer, to impart tackiness and adhesiveness, which adheres strongly to assure a tenacious lubricant film.

The Non-Newtonian behavior of these lubricants have shown greater reduction in friction and wear due to maintaining greater film thickness on gear teeth, thereby reducing amperage consumption, as well as reducing frictional heat.

Non-Toxic Gear Oil Series meets all the FDA requirements for qualification as a white mineral oil (FDA Regulation 21 CFR 172.878) and means that the fluid maybe used in lubricants for incidental contact with food as specified in 21 CFR 178.3570.  This regulation qualifies lubricants as a candidate for NSF rating H-1 for incidental food contact in meat and poultry plants.  The additives used in formulating Non-Toxic Gear Oil Series also meet all the requirements under Regulation 21CFR 178.3570.

TO ORDER or FOR ADDITIONAL INFORMATION

S-NT-GO Series

FOOD GRADE GEAR OIL

TYPICAL  CHARACTERISTICS

NON TOXIC GEAR OIL          75   	 80  		75/80			    75/90  			  80/90 	  90		  90/140		    140		   250	   ASTM METHOD

ISO Viscosity Grade	   32	 46	   68		 		100				 	150	 220	   320		 460		  680			D-   2422

AGMA Lubricant Number	1EP        	  2EP           	   		3EP		 	4EP            5EP                 6EP             	 7EP	    8EP

Viscosity cSt @ 100C	  6                      8                     10                   			14                     		18                  23                  29                  	37             		48	  	D-     445

@   40C                  32   	             46                    68	          		100	            		150               220                320                 	460               680	  	D-     445

Viscosity Index                               133                 146                   131                 			142                    		124              124                124                 		124               124	  	D-   2270

Pour Point C (F)                       -48(-55)          -46(-50)	    -43(-45)          	-40(-40)		-37(-35)       -34(-30)          -32(-25)            -29(-20)       -26(-15)               	D-       97

Flash Point C (F)                     231(448)         233(451)         236(457)         	249(480)             250(482)      254(490)        270(518)           280(535)      280(535)              	D-       92

Foam Sequence I, II, III               --------------------------------------------------------------------------- Pass -----------------------------------------------------------------------------		D-     892

Demulsibility 82C                      ----------------------------------------------------------------------- 40/40/0(30) ------------------------------------------------------------------------            	D-   1401

Four Ball Wear, mm 40kg, 1200 rpm, 75°C (1hr)---------------------------------------------------------- 34 -----------------------------------------------------------------------------	 	D-   2266

Copper Corrosion 121C (250F), 3 hrs ----------------------------------------------------------------------1a------------------------------------------------------------------------------            	D-     130

Rust Test                                         ---------------------------------------------------------------------------Pass-----------------------------------------------------------------------------            	D-665AB

Gear Test, FZG, SPUR, Stage Pass -------------------------------------------------------------------------- 12+ ----------------------------------------------------------------------------

Timken OK Load kg / (lb)             -------------------------------------------------------------------------- 45+ (100) ----------------------------------------------------------------------            		D-    2509

Food Grade Status	             ---------------------------------------------------------------------------  H-1 ----------------------------------------------------------------------------		NSF

NSF Registration	          130827           130828        130835           130834            130833         130832          130831           130830        130829

PIN#	07525	     07520          07515              07510              07518           07522            07500             07505	07530

TO ORDER OR FOR ADDITIONAL INFORMATION