PRODUCT  DATA  SHEET

G

###### S-ALO #5

AIRLINE LUBRICANT

PRODUCT  DESCRIPTION

\

Sentinel® S-ALO #5 is an exclusive formulation designed for the lubrication of airlines.  Its unique formulation offers the capability of encapsulating “moisture”. S-ALO #5 has the ability of absorbing more than 20% of its weight in water because of this exclusive compounding the water become part of the lubricant, holding it in permanent suspension.  The emulsifier within the lubricant forms a stable and permanent oil and water emulsion with a high lubricity factor.

TYPICAL  CHARACTERISTICS

Sentinel® incorporates special corrosion additives to eliminate oxidation and rust within the tools.

Sentinel® S-ALO #5 is a clean, ashless, residue free fluid that cleans as it lubricates to maintain airflow free from blockage, while assuring maximum “wetting” action of all metallic surfaces for reducing wear, tear and deterioration of expensive equipment.

ISO Viscosity Grade	46					ASTM D-2422

Viscosity cSt @ 100˚C	8  					ASTM D-  445

@   40˚C	46

Viscosity Index        	146					ASTM D-2270

Pour Point ˚C (˚F)	-40 (-40)					ASTM D-    97

Flash Point ˚C (˚F)	232 (450)					ASTM D-    92

Foam Sequence I, II, III	Pass					ASTM D-  892

Copper Corrosion

121˚C (250˚F), 3 hrs.	1a					ASTM D-  130

Rust Test	Pass					ASTM D-  665A&B

Appearance     	Golden

PIN #						08105

TO ORDER or FOR ADDITIONAL INFORMATION