PRODUCT  DATA  SHEET

G

###### S-RC #1

ROLLER CHAIN OIL

PRODUCT  DESCRIPTION

S-RC #1 is a blended synthetic metallic roller chain lubricant.  An exclusive Sentinel® formulation of synthetic fluids with a metallic additive package containing a high homogenized submicron particle sized self-lubricating metallic solids.

The carrier will act just as a medium to carry the solids and deposit them into all internal working areas of the chains to guarantee maximum reduction of friction and subsequently elimination of wear.

The metallic solids, including molybdenum disulfide, beryllium and titanium, will provide exceptional anti-wear protection in those areas of the chain (rollers and pins) that are subjected to the heaviest operational wear.  The non-oily carrier will assure maximum cleanliness, providing adequate corrosion protection and water displacement while acting as a rust and corrosion preventative.

TYPICAL  CHARACTERISTICS

While pins, bushings, sprockets and links will be properly lubricated, the clean outside surface of the chain will not be subject to contamination of dirt, dust, powder, lint or any other foreign particles found in the environment.  No scuffing, gouging or wear will appear, S-RC #1 is a superior lubricant that will eliminate the problems of grease lubrication and conventional lubricating oils where the actual lubricated surfaces are the exterior of the chains where wear will not be apparent although the grease or oil will act as a magnet holding sand, dust or any other abrasive materials that will actually accelerate the wear and tear on the moving surfaces.

Viscosity cSt @ 100˚C	3.6

@  40˚C	13.7					ASTM D   445

Viscosity Index   	144 					ASTM D-2270

Pour Point ˚C (˚F)	-48(-50)					ASTM D-    97

Flash Point ˚C (˚F)  	93(200)					ASTM D-    92

Fire Point ˚C (˚F) 	133(271)					ASTM D-    92

Foam Sequence I, II, III	Nil					ASTM D-  892

Copper Corrosion, 121˚C (250˚F)

3 Hours	1a

Rust Test	Pass 					ASTM D-665 A & B

PIN #						08010

TO ORDER or FOR ADDITIONAL INFORMATION