PRODUCT DATA SHEET

G

###### S NT HO 10 W/S

NON-TOXIC

WATER SOLUBLE

HYDRAULIC OIL

PRODUCT  DESCRIPTION

S-NT-HO 10 WS is a special non-toxic, anti-wear, water soluble, highly refined, water white blend of U.S.P. fluids treated with synthetic compounds to produce a stable high film strength hydraulic fluid surpassing the highest purity standards.

S-NT-HO 10 WS offers superior protection against corrosion, rubber swelling and foaming.

S-NT-HO 10 WS meets all the FDA requirements for qualification as a white mineral oil (FDA Regulation 21 CFR 172.878) and means that the fluid maybe used in lubricants for incidental contact with food as specified in 21 CFR 178.3570.

The additives used in formulating S-NT-HO 10 WS also meet all the requirements under Regulation 21 CFR 178.3570.

TYPICAL  CHARACTERISTICS

ISO Viscosity Grade	32					ASTM D-2422

SAE Viscosity Grade	10					SAE J-300

Viscosity cSt @ 100˚C	6					ASTM D-  445

@   40˚C	32

Viscosity Index        	141					ASTM D-2270

Pour Point ˚C (˚F)	-40 (-40)					ASTM D-    97

Flash Point ˚C (˚F)	232 (450)					ASTM D-    92

Fire Point ˚C (˚F)	226 (438)					ASTM D-    92

Foam Sequence I, II, III	Nil					ASTM D-  892

Copper Corrosion

121˚C (250˚F), 3 hrs.	1b					ASTM D-  130

Rust Test	Pass					ASTM D-  665A&B

USDA Rating	H-3

Appearance    	Clear

PIN #						10505

TO ORDER or FOR ADDITIONAL INFORMATION