PRODUCT  DATA  SHEET

G

S NT AA1 OIL

NON-TOXIC GENERAL

PURPOSE EDIBLE OILS

PRODUCT  DESCRIPTION

S-NT-AA1 Oil Series is a special, highly refined, water white blend of U.S.P. fluid treated with synthetic compounds to produce a stable high film strength lubricant surpassing the highest purity standards.  S-NT-AA1 Oil Series is formulated to comply with FDA requirements for use in food, drug and cosmetic industries.

It is approved by the USDA and NSF with an H-1 rating for incidental contact with food products in Federally Inspected Meat and Poultry Plants.  It surpasses all U.S.P. requirements, and is, therefore acceptable for internal ingestion.

S-NT-AA1 Oil Series is free of unsaturated components and possesses a high degree of chemical stability.  It is suitable for plain and ball bearing applications where non-toxic oil are required.  It can be applied by drip cup, mist spray, brush or other mechanical means.

TO ORDER or FOR ADDITIONAL INFORMATION

###### S NT AA1 OIL

NON-TOXIC GENERAL

PURPOSE EDIBLE OILS

TYPICAL  CHARACTERISTICS

S-NT-AA1 Oil	         0			2		   5		      7		       10		   10W20	         20	      30	            40	            90	         90/140	   	140	    		250			ASTM METHOD

ISO Viscosity Grade       7			   10		  15	        22	         32	        46	       68		      100            150	        220	     	     320		    460	       		 680		           D-2422

AGMA Number	   	          0		            0		    0		        0 	          0               1	       2		        3	        4	             5	      	      6			  7				      8

Viscosity cSt@100°C    2.2	          2.8		  3.8		      4.6	         5.9     	  7.6	      9.5	   	    13              17	      22	             29		     37			  	  48	             D-445

@  40°C     7			   10		   15	  	   22		        32	        46	       68	   	   100	       150	     220	    	     320	        460	            680

Viscosity index			       125	         129  	  151		      127	         130          139	      119		       127	       122	     121	        	  123	    	 122		         121          	    D-2270

Pour Point °C(°F)	     -57(-70)   -54(-65)   -51(-60)	  -48(-55)    -46(-50)   -43(-45)    -40(-40)    -37(-35)    -34(-30)    -32(-25)		  -29(-20)	  -26(-15)		  -21(-10)     	    D-97

Flash Point °C(°F)   164(327)  164(327)  204(400)  210(410)  210(410)  220(425)   225(437) 	227(440)   243(469)  250(482)   264(507)	  288(550)	  228(550)		    D-92

Foam Sequence		      ----------------------------------------------------------------------------PASS----------------------------------------------------------------------------------        D-892

Rust Test			      ----------------------------------------------------------------------------PASS----------------------------------------------------------------------------------        D-665A&B

Food Grade Status     -----------------------------------------------------------------------------H-1-----------------------------------------------------------------------------------	       NSF

Color observed			    ----------------------------------------------------------------------Clear and Bright---------------------------------------------------------------------------

NSF Registration	------	------	     ------         ------      133557     133558     133559     133560      133561      133562      133563      133564      133565

PIN #                         17490     17495	  17497       17498        17500       17524	17503	  17505	      17507        17513        17517	  17515	     17520

TO ORDER or FOR ADDITIONAL INFORMATION