PRODUCT  DATA  SHEET

G

SL-C

LOW TEMPERATURE

CRYOGENIC LUBRICANT

PRODUCT  DESCRIPTION

SL-C is Sentinel’s answer to the need for a grease, which is outstanding for every phase of greasing in sub-zero operating conditions.  Sentinel’s SL-C Blended Synthetic grease is formulated to pump effectively – utilizing standard greasing equipment – in temperatures down to -73˚C (-100˚F).

Sentinel’s SL-C grease will resist water washout and it is extremely effective in preventing wear under higher

operating pressures and conditions found in heavily-loaded construction equipment, due to its synthetic metallic compounding, high film strength and “plating” properties.

Therefore, SL-C is recommended for multi-purpose lubrication for all types of machinery, bearings, slides, cams, ways, etc., being especially suited for uses in sub-zero/arctic conditions.

TYPICAL  CHARACTERISTICS

NLGI Grade			1					ASTM D-1092

Worked Penetration		310-340					ASTM D-  217

Dropping Point		None 					ASTM D-2265

Oxidation Stability 		-2					ASTM D-  942

Psi Drop @ 100 hrs

Rust Preventative		1a					ASTM D-1743

Water Washout		-1					ASTM D-1264

Extreme Pressure		36+ (80)					ASTM D-2509

Timken OK Load Kg (Lb)

Four Ball Wear		.6mm					ASTM D-2266

Solids		MoS2

USDA Rating		H-2

Appearance 		Opaque

PIN #								06010

TO ORDER or FOR ADDITIONAL INFORMATION