PRODUCT  DATA  SHEET

G

ANTI-SEIZE

EXTREME PRESSURE

PRODUCT  DESCRIPTION

Sentinel’s Anti-Seize is a synthetic multi-purpose E.P. Lubricant. It may be used in production machinery (sliding surfaces of reciprocating parts), machine shops, tool and die manufacturing, chemical industry applications, metal working and general industry.  Sentinel’s Anti-Seize will prevent corrosion and provide excellent lubrication on parts exposed to water, steam and most acids or alkalis.

Sentinel’s Anti-Seize is a highly concentrated, stable, non-melting molybdenum disulfide compound.  It is impervious to water and is not affected by most acids or alkalis.

Sentinel’s Anti-Seize has excellent lubricating qualities from -150˚C (-300˚F) to over 954˚C (1750˚F).  It has a high film strength, low coefficient of friction and a tenacious adherence to metal surfaces.

Sentinel’s Anti-Seize reduces wear and prevents seizing and galling on all extreme applications.

TYPICAL  CHARACTERISTICS

NLGI Grade			3					ASTM D-1092

Worked Penetration		220-250					ASTM D-  217

Dropping Point		None 					ASTM D-2265

Oxidation Stability 		-1					ASTM D-  942

Psi Drop @ 100 hrs

Rust Preventative		1a					ASTM D-1743

Water Washout		0.8					ASTM D-1264

Extreme Pressure		50+ (110)					ASTM D-2509

Timken OK Load Kg (Lb)

Four Ball Wear		.5mm					ASTM D-2266

Solids		MoS2

USDA Rating		H-2

Appearance 		Dark Metallic

PIN #							       03193

TO ORDER or FOR ADDITIONAL INFORMATION