PRODUCT  DATA  SHEET

###### SL-RCG

RUBBER COMPATIBLE

GREASE

G

PRODUCT  DESCRIPTION

SL-RCG is rubber compatible grease specifically formulated and designed to operate as multi-purpose grease without having the usual effects that greases have when in contact with rubber seals and “O” rings.

It is completely compatible with the following rubber materials: natural, Buna S, Buna N, and neoprene.

Effects on Rubber 5 Days (120 hrs.) @ 158°F

Natural		Buna S	Buna N		Butyl	Neoprene

% Linear Swell	0.35		0.7		0.7	1.5	0.0

Hardness		-2			-2		  +2	+4		-2

Operating Range											    -50  to  +325

Color											       Light Tan

TYPICAL  CHARACTERISTICS

NLGI Grade         	2 					ASTM D-1092

Worked Penetration	265-295					ASTM D-  217

Dropping Point	None  					ASTM D-2265

Oxidation Stability

Psi drop @ 100 hrs	-1					ASTM D-  942

Rust Preventative	1a					ASTM D-1743

No Stain

Water Washout	1					ASTM D-1264

Extreme Pressure	34+ (75)					ASTM D-2509

Timken OK Load Kg (Lb)

Four Ball Wear	.6 mm					ASTM D-2266

Appearance	Light Tan

PIN #		                                                             03010

TO ORDER or FOR ADDITIONAL INFORMATION