.

PRODUCT  DATA  SHEET

###### SL-SR33

SOLVENT RESISTANT

GREASE

PRODUCT  DESCRIPTION

A fully synthetic solvent resistance grease for all types of bearings operating under extreme chemical attack.  Totally resistant to kerosene, naphtha, perclorethlene, mineral oils and most types of hydrocarbon solvents.

TYPICAL  CHARACTERISTICS

Good protection against carbon tetrachloride and xylene.  Useable as a good rust and oxidation protective film.  Used in many chemical industries.

NLGI Grade         	2 ½					ASTM D-1092

Worked Penetration	250-275					ASTM D-  217

Dropping Point	None  					ASTM D-2265

Oxidation Stability

Psi drop @ 100 hrs	-1					ASTM D-  942

Rust Preventative	1a					ASTM D-1743

No Stain

Water Washout	1					ASTM D-1264

Extreme Pressure	34+ (75)					ASTM D-2509

Timken OK Load Kg (Lb)

Four Ball Wear	.6 mm					ASTM D-2266

Appearance	Amber

PIN #							03001

TO ORDER or FOR ADDITIONAL INFORMATION