PRODUCT  DATA  SHEET

###### SEN-NO-FREEZE

ADVANCED FORMULA SYNTHETIC ANTIFREEZE

PRODUCT  DESCRIPTION

SEN-NO-FREEZE provides optimum rust and corrosion protection of your cooling system.  It is recommended for the cooling system of passenger cars, trucks, tractors, stationary equipment, and air conditioning towers where recirculating water will be left in the system during winter.  SEN-NO-FREEZE is formulated to keep pH balance of your cooling system and maintain adequate protection of rust and corrosion with minimum cost.  It is harmless to rubber hoses, water pumps, and gasket material.

SEN-NO-FREEZE meets and exceeds requirements of the SAE, ASTM and CSMA.  SEN-NO-FREEZE is compatible with all nationally distributed water filter elements except the chromate type and is completely miscible with water.  SEN-NO-FREEZE contains biocides that will destroy living organisms in standing water.

An important property of SEN-NO-FREEZE is its ability to lower the freezing point of water.  This results in its use in the formulation of anti-freeze mixtures.  SEN-NO-FREEZE is about 90% as efficient as Ethylene Glycol in anti-freeze applications, but it is much less toxic.  It is frequently used where toxicity is a consideration.  SEN-NO-FREEZE is non-corrosive and non-toxic.  It has a low vapor pressure and high flash point.  It is easily handled in ordinary commercial conditions.

NOTE: Sentinel’s® SEN-NO-FREEZE should not be used in concentrate form – 68% give maximum freezing protection -92°F (-69°C).  A concentration range of 50 to 70% will increase it 25°F (-4°C), thus providing a significant margin of safety against boiling and overheating.

TYPICAL  CHARACTERISTICS

Ash Content           							1.2%

pH, 33% by Volume Solution							10.2

50% by Volume Solution							10.2

Reserve Alkalinity							14.6

Specific Gravity at 68°F/68°F

33% by Volume Solution							1.045

50% by Volume Solution							1.073

Concentrated							1.124

Distillation Range Concentrated, Initial Boiling Point						                 242°F (117°C)

Dry Point (Final Boiling Point)							406°F (208°C)

Freezing Point and Boiling Point			FP					         BP

33% by Volume Solution	-1.05°F (-18.3°C)					220°F (104°C)

40% by Volume Solution	-12.0°F (-24.4°C)					222°F (106°C)

50% by Volume Solution	-34.0°F (-36.7°C)					227°F (108°C)

60% by Volume Solution	-64.0°F (-53.3°C)					232°F (111°C)

70% by Volume Solution	-84.0°F (-64.4°C)					239°F (115°C)

Concentrated	- 5.0°F (-20.6°C)					323°F (162°C)

Flash Point (Tag Open Cup), 70% by Volume Solution 		None

Concentrated				246°F

Average Net Weight per Gallon @ 60°F (16°C)				9.4 pounds (4.26 Kg)

Appearance				Golden Yellow

TO ORDER or FOR ADDITIONAL INFORMATION

PIN #    						02120