PRODUCT  DATA  SHEET

G

SLC 2

STROKE

TWO STROKE OIL

PRODUCT  DESCRIPTION

Sentinel’s® 2 Stroke is a unique, premium quality synthetic two cycle engine lubricant specifically for use in two strokes engines at fuel-to-oil ratios of up to 100 to 1.

Additionally, SLC 2 Stroke was tested in this same procedure at one-half the level of lubricant prescribed for TC-W evaluations.  Even at this lean ratio, SLC 2 Stroke met all the requirements of the TC-W oil test procedure.  In fact SLC 2 Stroke was the first two stroke lubricant to achieve outstanding performance.

In addition to achieving outstanding results in the engine tests, SLC 2 Stroke has successfully passed the BIA tests for rust protection and for fuel miscibility.

TYPICAL  CHARACTERISTICS

SLC 2 Stroke has a very low pour point (-40°F) which, together with its stable pre-mix properties, minimizes storage and handling.

When using SLC 2 Stroke at one-half the normal oil concentration, the two stroke engine operator should observe easier starting, higher power output and less smoke emissions.  Although the effect of two stroke lubricants on the ecology has not yet been well defined, the synthetic component of SLC 2 Stroke inherently possess superior “Biodegradability” properties

This “third generation” two stroke engine fluid employs new and unique synthetic technology developed exclusively by Sentinel® Lubricants Corp.  Its conventional ash less dispersant and other additives have all been proven in both extensive engine testing and field experience.

Viscosities, cSt 100°C	8.2					ASTM D-445

Viscosity Index	121					ASTM D-2270

Pour Point °C (°F)	-40 (-40)					ASTM D-97

Flash Point °C (°F)	94 (201)					ASTM D-92

Color     		Blue Green

Ash Content	Ashless

PIN #						18500

TO ORDER or FOR ADDITIONAL INFORMATION