PRODUCT  DATA  SHEET

G

###### S-1000 HT

EXTREME HIGH

TEMPERATURE OIL

PRODUCT  DESCRIPTION

Sentinel’s S-1000 HT is a synthetic high temperature lubricant designed primarily for high temperature equipment, such as oven chains and tenter frames as well as paint ceramic currying ovens and bearing lubrication.

Formulated from quality synthetic base stock and additives systems, S-1000 HT provides the following performance benefits.

● Excellent resistance to high temperature oxidation and high thermal stability for prolonging lubricant life.

● Superior anti-wear properties for reduce drag.

● Extremely low volatility resulting in less oil    consumption.

● High viscosity index allows functional viscosities to be maintained at higher temperatures.

Sludge and carbon deposits are significantly reduced because this “carbon buildup” is eliminated.  In fact, this oil will in time remove any carbon already deposited on the chain.

TYPICAL  CHARACTERISTICS

ISO Viscosity Grade	           				1500

Viscosity cSt  @100˚C        				100 				ASTM D-  445

@  40˚C				1550

Viscosity Index				161		ASTM D-2270

Pour Point ˚C (˚F)   	       		 -20 (- 5)		ASTM D-    97

Flash Point ˚C (˚F)             				310 (590)                    	ASTM D-    92

Fire Point ˚C (˚F) 	      				415 (779)

Evaporation Loss, 22 hrs, at 98.9°C, %		0.10		ASTM D-  972

Four Ball Wear, mm 40kg, 1200 rpm, 1 hr., 75˚C  		0.45		ASTM D-2266

Total Acid No., mg KOH/g <0.01		< 0.01 		ASTM D-  974

Noack Volatility, 250 ˚C, 1 hr, %wt. Evap.		0.6		DIN        51581

Food Grade Status			H1		NSF

NSF Registration			136606

PIN #	          	  		16079

TO ORDER or FOR ADDITIONAL INFORMATION