PRODUCT  DATA  SHEET

###### SULCO 5W20

SYNTHETIC

AIR COMPRESSOR

LUBRICANT

PRODUCT  DESCRIPTION

Sentinel’s Synthetic Sulco 5W20 compressor lubricant has been specially formulated for use in rotary screw air compressor.  Sentinel’s Sulco 5W20 compressor lubricant is a blend of polyalkylene glycol and polyol ester and thus takes advantage of the excellent performance attributes of both classes of compound.

Sulco offers improved electrometric seal compatibility.        Sulco does not suffer from shrinkage commonly encountered when using conventional lubricants, nor does it swell excessively as compared to when diester lubricants are used.

PRODUCT  ADVANTAGES

Sulco has inherently high viscosity index of Sentinel’s Sulco 5W20 lubricant no additional VI improvers are added to the formulation.  Thus the product remains stable to shear forces and does not suffer any irreversible effects.

Sulco meets the SAE 5W-20 classification, as a result cold weather start ups are easier and less energy is required.  Its high viscosity index is equivalent to a 20 weight fluid at normal operation temperatures.

Extended drain intervals

Extended oil separator service intervals

Fewer air filter changes

Improved compressor efficiencies

Less downtime

Reduced feed rates

Reduced oil carryover

Reduced vapor pressure

Reduced equipment operational problems

Reduced oil consumption

Reduced maintenance costs

Improved safety

Eliminates seasonal oil change

Excellent high temperature stability

Improved oxidation stability

Energy conservation

Less oil carryover

Cooler running

Excellent electrometric

Seal compatibility

Hydrolytically stable

TO ORDER or FOR ADDITIONAL INFORMATION

Biodegradable

PRODUCT  DATA  SHEET

SULCO 5W 20

SYNTHETIC

AIR COMPRESSOR

LUBRICANT

TYPICAL  CHARACTERISTICS

5 W 20	  				  	ASTM METHOD

Viscosity cSt @ 40°C		     47.07 cSt	                  		       ASTM - 445

@ 100°C		      8.93 cSt                                                                 ASTM - 445

Viscosity Index		     173	                  		      ASTM D- 2270

Density                                                                  0.989 g/cm3	 		      ASTM D- 1298

Flash Point °C (°F)		    >260˚C	                  		      ASTM D- 92

Foam Tendency		     Nil	                   		      ASTM D- 892

Barium content                              		     Nil                                                                         ASTM - 4951

Nitrogen content                                                    Nil                                                    	        ASTM - 4951

Maximum operating temperature                         200˚C

Pour Point                                                    		   <-50˚C                                                                    ASTM D- 97

Flammability Point                                      Not routinely recorded                                                   ASTM D- 2115

Appearance				         Clear Amber

PIN #												    14605

TO ORDER or FOR ADDITIONAL INFORMATION