PRODUCT  DATA  SHEET

G

###### SCH

LOW TEMPERATURE

CRYOGENIC

HYDRAULIC OIL

PRODUCT  DESCRIPTION

SCH Cryogenic Hydraulic Oil is especially prepared to meet the needs of systems that must operate through wide ranges of temperature.  This “all weather” efficiency makes SCH especially suitable for sub-zero operating conditions.

SCH has a “High V.I.” (Viscosity Index), which has the advantages of a stable, uniform viscosity, whether at extreme cold or elevated temperature operating conditions.  It is not handicapped by the usual thickening when extremely cold, or serious thinning, plus leakage at high temperatures.  This means a more uniform functioning of the hydraulic system throughout the year, without the need for seasonal oil changes.

SCH is carefully formulated for long-lasting oxidation resistance against sludging; it is non-foaming; it has excellent lubrication characteristics, which reduce friction and prevent wear of delicate hydraulic elements and low pour points, without congealing, therefore giving it the ability of handling greater loads under all conditions.  It is compatible with all seals, gaskets and “O” rings.

SCH can also find use as a lubricant as well hydraulic fluid where increase in torque because of thickening lubricant cannot be tolerated.  For example, fine instruments and other mechanisms where power input is limited.

TYPICAL  CHARACTERISTICS

ISO Viscosity Grade	15					ASTM D-2422

AGMA Lubricant Number 	---

Viscosity cSt @ 100˚C	3.6					ASTM D-  445

@   40˚C	14.5

@  -40˚C	2025

Viscosity Index        	135					ASTM D-2270

Pour Point ˚C (˚F)	-84 (-100)					ASTM D-    97

Flash Point ˚C (˚F)	230 (446)					ASTM D-    92

Fire Point ˚C (˚F)	240 (460)					ASTM D-    92

Foam Sequence I, II, III	Nil					ASTM D-  892

Demulsibility 82˚C	40/40/0 (15)					ASTM D-1401

Four Ball Wear, mm 40 kg, 1200 rpm, 75˚C (1hr)	.38					ASTM D-2266

Copper Corrosion 121˚C (250˚F), 3 hrs.	1a					ASTM D-  130

Rust Test	Pass					ASTM D-  665 A & B

FZG, Gear Test, Spur, Stage Pass	12+

Timken OK Load Kg (Lb)	36+ (80)					ASTM D-2509

USDA Rating	H-2

PIN #						13030

TO ORDER or FOR ADDITIONAL INFORMATION