PRODUCT  DATA  SHEET

###### MOLY DRY FILM

MOLY DRY FILM

PRODUCT  DESCRIPTION

Sentinel’s Moly Dry Film is an extra fine Molybdenum Disulfide with a controlled PH.  It meets MIL Spec no. 7866B-B.  It is designed to prevent seizing, galling, and pitting, and also rust and corrosion.  When Sprayed on metal surfaces and burnished in, it has a tendency to plate onto the metal surface as a fine, dry, lubricant with a high film strength, and excellent lubricity.  It resists acids, water, and solvents.  It will not cause rust and corrosion, will not fly off or wash off.

Sentinel’s Moly Dry Film is designed to be used on threads, plug bolts, etc…, in high temperatures, as a break in lubricant, on sliding surfaces, on open gears in contaminated environments, such as dust, flour, lint, paper, etc…Specially recommended on cross screws for tenter frames, and break in periods.

TYPICAL  SPECIFICATIONS

Product                                                                                				MOS2

Particle Size					Submicron

Moisture Content					Zero

Film Strength					400,00 P.S.I.

Temp Range °F					Cryogenic to 750 in air							2000 in the vacuum of space

Melting Point °F					4370

Physical Structure		                                 Lamellar Solid

PIN #					12500

TO ORDER or FOR ADDITIONAL INFORMATION