PRODUCT  DATA  SHEET

G

###### S-10/50

###### WAY OIL

WAY LUBRICANTS

PRODUCT  DESCRIPTION

Sentinel’s line of Way Oils are blended from high quality, synthetically treated base oils, a superior combination of extreme pressure, anti-wear, rust and oxidation inhibitors.  In addition these oils are fortified with oiliness and special stringiness additives to impart tackiness and adhesiveness.

Sentinel’s Way Oils adheres strongly to sliding metal surfaces and provide a tenacious lubricant.  The tackiness combined with exceptional lubricity offers ideal lubrication for vertical as well as horizontal ways.

TYPICAL  CHARACTERISTICS

The low coefficient of friction overcomes the stick-slip motion associated with slow moving machine parts even after standing overnight.  They are highly effective in controlling wear and protecting against galling.

Typical applications include sliding ways of machines including lathes, planers, shapers, drilling and tapping machines, grinders, boring machines, jig borers, milling machines and other applications requiring an adhesive, non-drip characteristic lubricant, such as enclosed gears and all types of industrial plain and anti-friction bearings.

Application methods are an oil can, oil cup, reservoir, splash, or by automatic dispensing equipment.

Viscosity cSt @ 100˚C	18					ASTM D-  445

@   40˚C	100

Viscosity Index        	199					ASTM D-2270

Pour Point ˚C (˚F)	-29 (-20)					ASTM D-    97

Flash Point ˚C (˚F)	200 (428)					ASTM D-    92

Fire Point COC ˚F	450					ASTM D-    92

Rust Test	Pass					ASTM D-  665 A & B

Conradson Carbon Residue (Base Oil)	0.05					ASTM D-  189

Timken OK Load kg/ (lb)	36+ (80)					ASTM D-2509

Appearance  	Light Green

PIN #						     12270

TO ORDER or FOR ADDITIONAL INFORMATION