PRODUCT DATA SHEET

G

###### SPINDLE

###### OIL Series

PRODUCT  DESCRIPTION

Sentinel’s non-newtonian spindle oils have been scientifically blended with EP and rust and oxidation additives to reduce friction and wear, thereby reducing amperage as well as frictional heat.  These fluids are non-staining, non-corrosive with virtually no odor, specifically developed for the knitting industries as a lint-free oil.

PRODUCT  ADVANTAGES

Sentinel’s special spindle oils will be pulled into the spindle bearing and gears, they will penetrate and lubricate pins in chains and will not drip off or be absorbed as quickly as conventional oils.  These fluids will extend lubrication intervals and provide superior lubrication through normal cycles.  As a lubricant the long chain molecules will reduce wear and increase tool life up 50% by wrapping around the spindle bearing and clutches to provide bounding film lubrication.

Extend Lubrication Cycle

Non-Foaming

Non-Staining

Reduced Maintenance Cost

Improved Efficiencies

Improved Safety

Improved Oxidation Stability

Cooler Running

TO ORDER or FOR ADDITIONAL INFORMATION

###### SPINDLE

###### OIL Series

TYPICAL  CHARACTERISTICS

L				LM	  		M	  M-M  					  H			ASTM METHOD

ISO Viscosity Grade	     	2	 		10	  	22		      32		    46			D-   2422

Viscosity cSt  @ 100C	     	1.5		2.1		3.9		      5.7		  7.7			D-     445

@   40C	  		5.5	7.19		        17			    31			  46		        D-     445

Pour Point C (F)                 	-73(-100)       	-63(-80)	  	   -51(-60)           -48(-55)		    -43(-45)	    D-       97

Flash Point C (F)                	   155(311)      	160(320)                 169(336)          180(356)          	             190(374)              D-       92

Foam Sequence I, II, III                                   -----------------------------------------------------Pass-------------------------------------------------             D-     892

Demulsibility, 54C (130˚F)                            -------------------------------------------------40/40/0(30)--------------------------------------------             D-   1401

Copper Corrosion 121C (250F), 3 hrs            ----------------------------------------------------1a----------------------------------------------------            D-     130

Rust Test                                                           ----------------------------------------------------Pass--------------------------------------------------             D-665A&B

Conradson Carbon                                            ----------------------------------------------------0.01--------------------------------------------------             D-     189

Appearance				        ------------------------------------------------Yellow Cast---------------------------------------------	     D-   1500

PIN#			        11500          		11503              	11505                 11507		11510

TO ORDER or FOR ADDITIONAL INFORMATION

###### SPINDLE

###### OIL Series

TYPICAL  CHARACTERISTICS

L				LM	  		M	  M-M  					  H			ASTM METHOD

Specific Gravity, g/ml @ 25C      0.7976	           0.807                0.814	   0.821	 0.827		 D-  1298

Viscosity Index	                 80       		 85	                    125		    120	                      135   		 D-   2270

Density, lb/gal @ 25C                    6.59                       6.69	      6.78                6.84		       6.89      	       D-  1298

TAN, mg/KOH/g                       ---------------------------------------------- 0.10 -------------------------------------------             D-    974

Evaporating Loss, 22hrs @ 40C  ------------------------------------------- 0.10 -------------------------------------------             D-    972

Operating Temperatures           -57C(-70F)        -54C(-60F)     -40C(-40F)   -40C(-40F)       -35C(-30F)

Intermittent                      to                           to                       to                     to                          to

60C(140F)         65C(149F)     70C(150F)     86C(176F)       86C(185F)

Surface Tension @ 100C dynes/cm   ---------------------------------------  23  --------------------------------------------

------- No Ash Content ------- No Saponification Value ------ No Fats in our Oils -------

PIN#			        11500          		11503              	11505                 11507		11510

TO ORDER or FOR ADDITIONAL INFORMATION