PRODUCT DATA SHEET

###### S-INERTA

###### PLUS FTG 2

###### PFAE CHEMICALLY

###### INERT GREASE

G

PRODUCT  DESCRIPTION

The widespread manufacture and use of aggressive chemicals has resulted in a growing need for Sentinel’s S-INERTA PLUS chemical inert greases.  They have proven to be a safe and cost-effective in many applications where other lubricants are not recommended because of the danger of rapid reaction, ignition or explosion.

S-INERTA PLUS are high performance, creamy, homogenous, white greases, based on Perfluoropolyether (PFAE) and thickened with Polytetrafluoroethylene (PTFE) making them stable and chemical resistant.

Sentinel’s S-INERTA PLUS are inert and do not react even at high temperatures with fuels, acids, inorganic alkalis, halogens, fuming nitric acid and oxidizing solutions.

Sentinel’s S-INERTA PLUS are resistant to oxidation and to chemical agents, they are compatible with all types of materials (glass, metal, elastomers, plastomers, and ceramics).

TYPICAL  CHARACTERISTICS

Sentinel’s S-INERTA PLUS greases can be used in the presence of water, oil, and vapor (in general, with all organic substances which are highly fluorinated); without emulsifying.

Sentinel’s S-INERTA PLUS are thermally stable, they have no dropping point and can be used at high temperatures and in oxidizing conditions.

Sentinel’s S-INERTA PLUS is oxygen compatible.

Sentinel’s S-INERTA PLUS product advantages are:

Chemically Stable

Extreme high temperatures stability

Good low temperatures properties

Very good E.P. and wear characteristics

Good evaporative loss

Good viscosity indexes

NLGI Grade	2					      ASTM D-1092

Worked Penetration	265-295					      ASTM D-  217

Dropping Point	None					      ASTM D-2265

Service Temperature Range, ˚C (˚F)       	-35 to 260 (-25 To 500)					                                                     Corrosion Protection 	0/0				      	            DIN 51802

Evaporative loss

24 hours® 200˚C (%weight loss)	0.9					      ASTM D-  972

Specific Gravity @20˚C (g/cm3)	1.91					      ASTM D-  891

Base Oil Viscosity cSt@100˚C	40 					      ASTM D-  445

40˚C	420

Viscosity Index	144					      ASTM D-2270

Solids	Polytetrafluoroethylene

USDA Rating	H-2

Appearance	White

PIN #						              05202

TO ORDER or FOR ADDITIONAL INFORMATION