PRODUCT  DATA  SHEET

G

###### SL-VSG #2

VALVE STEM

SILICONE GREASE

PRODUCT  DESCRIPTION

SL-VSG #2 is a heavy-consistency, grease-like silicone paste designed as a valve lubricant and sealant that provides a non-curing moisture barrier.  This lubricant is used in lubricating plug valves, gate valves, ball valves, butterfly valves, automated valves, rubber and plastic O-rings; sealing vacuum and pressure systems (especially outdoor) equipment subjected to washing and harsh environments); damping medium for dash pots in electrical equipment.

It has a temperature range from -40° to 200°C (-40° to 400°F).

TYPICAL  CHARACTERISTICS

SL-VSG #2 has a heavy consistency; worked penetration of 260 maximum; non-melting; low volatility; high dielectric strength; moisture and ozone resistance; good thermal, oxidative chemicals (e.g. liquid chlorine, liquid oxygen) unless evaluated prior to use.

It may be applied by brushing, wiping or automated equipment.

NLGI Grade         								 2

Unworked Penetration			265-295

Worked 60, maximum							           260

Dropping Point	  						         None              Bleed 24 hr/200°C (392°F), %							          0.05

Evaporation, 24 hr/200°C (392°F), %							            1.1

Service Temperature Range, °C (°F)							-40 to 204

Melting Point   							         None

Specific Gravity at 25°C (77°F)       							            1.0

FDA Recognition, 21 CFR 175.300							           Yes

Electrical								-2

Dielectric Constant, at 100 Hz							          2.88

at 100 Hz							          2.95

Dissipation Factor, at 100 Hz							       0.0001

at 100Hz							    <0.0005

Dielectric Strength, volts/mil, 50 mil gap							         >450

Volume Resistivity at 23°C (73°F), ohm-cm						               2.17x10-15

Arc Resistance, seconds							           124

Dielectric Strength							           400 volts/mil

Vol. Resist.   1 x 1015 ohm cm

Appearance Visual						       Clear White, Translucent

PIN #		                                                                    03365

TO ORDER or FOR ADDITIONAL INFORMATION