### APPENDIX A

Mixing Instructions

RUST

ARREST

### TYPICAL VISCOSITY – DILUTION DATA

%SOLVENT	%NON-	 BROOKFIELD		SPINDLE

%RUST ARREST	ADDED	VOLATILE	 VISCOSITY @ 77°F CPS	NUMBER @ RPM

100			0		62		45,000	6	10

81			19		50		11,000	3	10

65			35		40			3,000	3	10

48			52		30		     	800		3	10

32			68		20		150		3	10

TYPICAL SALT FOG PERFORMANCE DATA HOURS

RUST ARREST – yields firm wax like coating

Dry Film				Rust Arrest

0.5 mil					800+

1.0 mil				     1500+

2.0 mil				     2000+

5.0 mil				     3000+

Salt Fog – Federal Standard 791B Method 4001.2.  Panels are judged by reading the face of the panel (not the edges). Failure occurs when more than 3 dots of rust, no one of which is larger than a millimeter in diameter, appear on the face of the panel.

Note:  Solvents with a boiling point between 310-340°F require a minimum of 72 hours of drying time prior to testing in the salt fog cabinet.

RUST

ARREST

### RUST ARREST DILUTION STABILITY

Values represent solvent separation in upper layer (ml/100ml)

###### Concentration		1 day	3 days	1 week		2 weeks	1 month		2 months		3 months

65					0		0		0				0			0			0			0

60					0		0		0				0			0		      .7			.7

55					0		0		0				0			.6		1.4			2.2

45					0		0		.7				.7			.7		3.0			4.5

35					0	 1.0	   1.1			1.9		3.1		6.5		 11.4

25					.7	1.1	1.5			2.2		4.5		9.0		 13.5

10					.7	1.2	2.2			5.8		8.8		 15.4		 27.2

RUST ARREST DIP FILM (DRY) VS VISCOSITY & NON-VOLATILE

###### Rust Arrest

% Non-Volatile

60%																  45000 CPS / 40 MILS

50%															   	11000 CPS / 9.0 MILS

40%																	 2000 CPS / 2.5 MILS

30%																		 800 CPS / 0.9 MILS

20%																	 	 150 CPS / 0.2 MILS

ALL VISCOSITIES ARE MEASURED VIA BROOKFIELD VISCOSIMETER.

ALL FILM THICKNESS MEASURED BY “TOOKE INSPECTION GAGE”.

Application to panel is accomplished in accordance with Fisher-Payne Dip Coater – Federal Standards 141a – Method 2121.  Rate of withdrawal is 4” per minute.  Not before 72 hours are the panels ready for exposure in the salt Fog and Humidity Cabinets.