PRODUCT  DATA  SHEET

G

###### S-FRH 46

FIRE RESISTANT

HYDRAULIC FLUID

PRODUCT  DESCRIPTION

Sentinel® S-FRH 46 is a high molecular weight, polyol ester base, synthetic fire resistant biodegradable hydraulic fluid; which is recommended for those hydraulic applications where potential fire hazard exists.  S-FRH 46 has high viscosity and viscosity index which make it useful in a wide range of industrial lubricant applications.

• Meets Mil H 83282 & all others

TYPICAL CHARACTERISTICS

S-FRH 46 base fluids contain a highly specialized additive system.  This additive system provides S-FRH 46 exceptional anti-wear, rust and oxidation inhibiting, corrosion inhibiting and demulsibility properties.

S-FRH 46, like any other synthetic fluid, under the proper circumstances will burn.  However, unlike some synthetic base fluids when burned, S-FRH 46 does not evolve large volumes of dense and noxious smoke and fumes.

ISO Viscosity Grade	46					ASTM D-2422

SAE Viscosity Number	20W					SAE J-300

AGMA Lubricant Number

Viscosity cSt @ 100˚C	9.6					ASTM D-  445

@ 40˚C 	47.5

Viscosity Index        	192					ASTM D-2270

Pour Point ˚C (˚F)	-4 (-20)					ASTM D-    97

Flash Point ˚C (˚F)	314 (595)     					ASTM D-    92

Fire Point ˚C (˚F)	372 (700)

Foam Sequence I, II, III	Pass					ASTM D-  892

Demulsibility 82˚C 	40-40-0 (15)					ASTM D-1401

Copper Corrosion

121˚C (250˚F), 3 hrs.	1a					ASTM D-  130

Rust Test	Pass					ASTM D-  665 A & B

USDA Rating   	H-2

Color Observed	Clear

PIN #					   	     10240

TO ORDER or FOR ADDITIONAL INFORMATION

PRODUCT DATA SHEET (continued)

G

###### S-FRH 46

FIRE  RESISTANT

HYDRAULIC  FLUID

CONVERSION  PROCEDURE

Converting from Other Polyol Ester Fluids,

Phosphates Esters or Oil-Synthetic Blends:

S-FRH 46 is compatible and miscible with polyol esters, phosphate esters, and oil-synthetic blends, as long as the used fluids are in good condition and contain no water.  Simply add S-FRH 46 to the system, or to completely convert, drain the oil fluid and recharge with S-FRH 46.  Flushing is not necessary.

To Convert from Water Containing Fluids:

Water containing fluids such as water glycols, invert emulsion and thickened high water content fluids must be thoroughly drained and the system flushed with S-FRH 46.  For optimum performance, the operational S-FRH 46 should have a water content of less than 1%.

To Convert from Petroleum Oil-Based Fluids:

Completely drain and recharge the system with S-FRH 46.  However, to preserve the highest degree of fire resistance, petroleum oil residual should be less than 5%.  Depending upon the system design, this may require a flush with

S-FRH 46 following the drain.  In all conversion, consideration should be given to the use of proper seals and hoses.  This is also an appropriate time for the cleaning and/or replacement of suction strainers and filter elements to ensure trouble free operation after changeover.

S-FRH 46 is compatible with all ferrous and non-ferrous metals and their alloys.  S-FRH 46 is also compatible with the following elastomers normally used with oil base hydraulic fluid.

Elastomers									Compatibility

Fluroro-elastomer (Vitron, Teflon)						Satisfactory

Nitrile Buna N								Satisfactory

Polyurethane				Satisfactory

Nylon				Satisfactory

Silicon Rubber				Satisfactory

Butyl				Satisfactory but with reduced life

Ethylene Propylene				Satisfactory but with reduced life

EP R				Satisfactory but with reduced life

Neoprene				Satisfactory but with reduced life

Low Nitrile Buna N				Satisfactory but with reduced life

TO ORDER or FOR ADDITIONAL INFORMATION