PRODUCT  DATA  SHEET

###### S-MPO OIL Series

MULTI-PURPOSE OIL

PRODUCT  DESCRIPTION

Sentinel S-MPO Multi-Purpose oil is a specially compounded synthetic oil to meet the needs of all types of industrial lubrication.

S-MPO Multi-Purpose oil offers a superior combination of oxidation inhibitors to prevent sludging and deposit formation; a high level of E.P. additives to meet severe wear protection requirements; foam suppressants to eliminate foaming; and finally a new polymer additive to arrest leakage and assure a strong bond to metal retention for maximum “grip” to all surfaces.  It will not drip-out, fling-out or run-out.

S-MPO gives superior protection against corrosion, rubber swelling and exhibits excellent water demulsibility characteristics.  These are the qualities that are required to assure efficient, trouble-free operation and extended drain intervals of the new high modern equipment of today.

TO ORDER or FOR ADDITIONAL INFORMATION

S-MPO Multi-Purpose oil has proved itself in applications such as:

- Bearings

- Gears

- Electric Motors

- Hydraulic Systems

- Low Speed Spindles

- Machine Tool ways

- Small Precision Gearing

- And many types of Chain  Conveyors (Not be used as crankcase or air compressor lubricant)

###### S-MPO OIL Series

MULTI-PURPOSE OIL

TYPICAL  CHARACTERISTICS

10	   20	             30	          10/50                40                 50

ISO Viscosity Grade	  32	   68		        100		      100                150	 	    220       				ASTM D-   2422

AGMA Lubricant Number	                      1   		             2                   3                    3                  4

Viscosity cSt @ 100C	                   5.6	          9	             12                 18                 16.3              21.3				ASTM D-     445

@   40C	                  32                68	            100	             100                 150	      220			ASTM D -    445

Viscosity Index		         114              107	         110	             180+ 	         111               113			ASTM D-   2270

Pour Point C (F)                            -40(-40)       -37(-35)	-34(-30)        -37(-35)         -32(-25)       -29(-20)			ASTM D-       97

Flash Point C (F)                          200(392)      210(410)      220(428)       230(446)        224(435)	     230(446)				ASTM D-       92

Demulsibility 82C                         --------------------------------------------40/40/0(30) --------------------------------------			ASTM D-   1401

Four Ball Wear, mm

40 kg, 1200       75˚C (1 hr)		-----------------------------------------------.5m---------------------------------------------		ASTM D-   2266

C				Copper Corrosion 121C(250F), 3 hrs --------------------------------------------1a-------------------------------------	ASTM D-     130

Rust Test                                         ------------------------------------------------Pass-------------------------------------------			ASTM D-665A&B

Timken OK Load kg/ (lb.)             ------------------------------------------------25 (55) ----------------------------------------				ASTM D-   2509

Conradson Carbon                         ------------------------------------------------0.05--------------------------------------------	ASTM D-     189

Appearance                                   ----------------------------------------------Light Green-------------------------------------

PIN #                                                    08045       08050          08055	   08076               08060          08065

TO ORDER or FOR ADDITIONAL INFORMATION