PRODUCT  DATA  SHEET

G

###### S.P.O.

PENETRATING OIL

PRODUCT  DESCRIPTION

This is a Penetrant, Rust Preventative and Metallic boundary coating lubricant:

- PENETRANT frees rusted pins, etc.

- LUBRICATES deeply into linkage to reduce friction on pins, rollers, bushings and other pressure surfaces.

- DEPOSITS and PLATES S.P.O. metallic solids which “roll the load” to all metal parts.

TYPICAL  CHARACTERISTICS

S.P.O features the above listed three exceptional, built-in qualities.  The ability to creep into the smallest openings, the coating to all parts of a magnetic rust preventative and the plating of all parts with S.P.O. metallic solids “roll the load” and withstand load pressure of over 100,000 psi – makes it the outstanding product it is.  It resists abrasion and contaminants plus 95% of all acids.

S.P.O. is a completely homogenous, colloidally blended compound, therefore needs no mixing to use it and it will not separate.  It is stable under all conditions, and can be used and applied within a temperature range of from -40˚C -40˚C (-40˚F) to 399˚C (750˚F)

Viscosity cSt @ 100˚C	2.9

@  40˚C	10.3					ASTM D   445

Viscosity Index   	138 					ASTM D-2270

Pour Point ˚C (˚F)	-54(-60)					ASTM D-    97

Flash Point ˚C (˚F)  	93(200)					ASTM D-    92

Fire Point ˚C (˚F) 	118(244)					ASTM D-    92

Foam Sequence I, II, III	Nil					ASTM D-  892

Copper Corrosion, 121˚C (250˚F)	1a

3 Hours

Rust Test	Pass 					ASTM D-665 A & B

PIN #							08000

TO ORDER or FOR ADDITIONAL INFORMATION