PRODUCT  DATA  SHEET

G

###### S-GEAR OIL Series

GEAR OIL SERIES

PRODUCT  DESCRIPTION

Sentinel® Special Synthetic Gear Oils are multi-purpose specially compounded molybdenum sulfide gear lubricants formulated to provide superior film strength and extreme pressure properties.  They are truly anti-friction, anti-wear, anti-leak, anti-foam gear oils.  Sentinel® Special Synthetic Gear Oils also surpass FZG stage 12, the highest rating that can be attained.  They can be used as make-up and refill lubricants in all types of enclosed gear mechanisms, including spur, herringbone, spiral, bevel and hypoid.  Sentinel® Gear Oil Series will also adequately meet and surpass requirements of heavy duty industrial transmissions and gear trains subject to high load and impact loads.

PRODUCT  ADVANTAGES

Sentinel® Special Synthetic Gear oils are formulated to greatly improve the viscosity temperature slope.  In other words, they reduce the change in viscosity with increase in temperature under isothermal conditions.  The non-Newtonian behavior of these lubricants have shown greater reduction in friction and wear due to maintaining greater film thickness on gear teeth, thereby reducing amperage consumption, as well as reducing frictional heat.

When severe rise in temperature is reached, these lubricants will carry greater loads because of the flatter viscosity temperature slope.  The non-Newtonian as well as the non-foaming properties of these lubricants practically eliminate all leakage.

- Extended drain intervals

- Superior demulsibility

- Non-foaming

- Seal compatible

- Less downtime

- Reduced equipment operational problems

- Reduced maintenance costs

- Improved Safety

- Improved oil leakage

- Eliminates seasonal oil change

- Exceptional high temperature stability

- Improved Oxidation Stability

- Energy Conservation

- Cooler running

TO ORDER or FOR ADDITIONAL INFORMATION

###### S-GEAR

###### OIL Series

GEAR OIL SERIES

TYPICAL  CHARACTERISTICS

S-75	S-80	  S-75/80		  S-75/90  		S-80/90		 S-90		S-90/140		    S-140		  S-250	   ASTM METHOD

ISO Viscosity Grade	     32	 46	  68		 100				 150		220	   320			 460		  680		D-   2422

AGMA Lubricant Number	 		1EP        	  2EP           	   3EP		 4EP				5EP				6EP		7EP			8EP

Viscosity cSt  @ 100C			 6		  8			10							14				18			23			29				37			48		D-     445

@   40C	 32	 	 46                 68	          100	            150               220                320               	460            680	  D-     445

Viscosity Index	133				146	131			142			124			124			124			124			124		D-   2270

Pour Point C (F)		-48(-55)			-46(-50)		-43(-45)			-40(-40)		-37(-35)			-34(-30)				-32(-25)	-29(-20)	-26(-15)			D-       97

Flash Point C (F)		231(448)	233(451)			236(457)					249(480)		250(482)				254(490)				270(518)		280(535)	280(535)		D-       92

Foam Sequence I, II, III               --------------------------------------------------------------------Pass-----------------------------------------------------------------		D-     892

Demulsibility 82C                      ---------------------------------------------------------------40/40/0(30)--------------------------------------------------------------		D-   1401

Four Ball Wear, mm 40kg, 1200 rpm, 75°C (1hr)-------------------------------------------------.34-------------------------------------------------------------------		D-   2266

Copper Corrosion 121C(250F), 3 hrs -------------------------------------------------------------1a-------------------------------------------------------------------		D-     130

Rust Test                                         ------------------------------------------------------------------Pass-----------------------------------------------------------------		D-665A&B

Gear Test, FZG, SPUR, Stage Pass -----------------------------------------------------------------12+------------------------------------------------------------------

Timken OK Load kg/(lb)           ----------------------------------------------------------------45+(100)-----------------------------------------------------------------		D-    2509

USDA Rating			---------------------------------------------------------------------H-2------------------------------------------------------------------

Appearance 	   ---------------------------------------------------------------Dark Grey ----------------------------------------------------------------

PIN                                         07049            07110           07050              07070                 07130          07170            07190            07210         07230

TO ORDER or FOR ADDITIONAL INFORMATION