PRODUCT  DATA  SHEET

G

###### S-NT-CH 10

NON-TOXIC CHAIN OIL

PRODUCT  DESCRIPTION

S-NT-CH 10 is a special, highly water white blend of U.S.P fluid treated with synthetic compounds to produce a stable high film strength lubricant surpassing the highest purity standards.

S-NT-CH 10 is fortified with a special food grade polymer, to impart tackiness and adhesiveness, which adheres strongly to assure a tenacious lubricant film.  S-NT-CH 10 will penetrate and lubricate over a wide temperature range.  Recommend for on both ferrous and non-ferrous metals at high temperatures and provides for low corrosion.

S-NT-CH 10 meets all the FDA requirements for qualification as a white mineral oil (FDA Regulation 21 CFR 172.878) and means that the fluid maybe used in lubricants for incidental contact with food as specified in 21 CFR 178.3570.  This regulation qualifies a lubricant as a candidate for USDA rating H-1 for incidental food contact in meat and poultry plants.  The additives used in formulating S-NT-CH 10 also meet all the requirements under Regulation 21 CFR 178.3570.

TYPICAL  CHARACTERISTICS

ISO Viscosity Grade	           			32					ASTM D-2422

SAE Viscosity Grade			10							SAE J-  300

Viscosity cSt @ 100˚C        				6						ASTM D-  445

@  40˚C			32

Viscosity Index				110				ASTM D-2270

Pour Point ˚C (˚F)   	       	 	-40 (-40)			ASTM D-    97

Flash Point ˚C (˚F)             				210 (410)				ASTM D-    92        Fire Point ˚C (˚F) 	      				440    				ASTM D-    92

Foam Sequence I, II, III				Nil					ASTM D-  892

Demulsibility, 54.4˚C (130˚F)			40 / 40 / 0 (15)			ASTM D-1401

Copper Corrosion,

121˚C  (250˚F) 3 hrs		1a 				ASTM D-  130

Rust Test			Pass				ASTMD-665A&B

USDA Classification             		H-1

Appearance			Clear, Tacky

PIN #	          					17701

TO ORDER or FOR ADDITIONAL INFORMATION