PRODUCT  DATA  SHEET

G

###### SSF #8 M

MOLY SEMI-FLUID

PRODUCT  DESCRIPTION

SSF #8 M is a unique synthetic semi-fluid lubricant containing a metallic solid additive, Molybdenum Disulfide.  The 0.02 micron molybdenum disulfide particles in

SSF #8 M will plate onto all surfaces and embed themselves to provide an extremely low coefficient of friction and high lubricity.

TYPICAL CHARACTERISTICS

SSF #8 M will not channel as greases normally do, and yet will retain itself as greases do and oils will not.  It possesses extreme pressure resistance of gear lubrication, as well as the softness for use in bearings, on slides, cams, open gears, etc. requiring only an extremely thin film to adequately lubricate these parts and keep the two metal surfaces separated.  Because of the foregoing, SSF #8 M has unlimited applications for use in leaky gearboxes where the speeds are not too great, on slides, open gears, cams, etc.

NLGI Grade			0					ASTM D-1092

Worked Penetration		355-385					ASTM D-  217

Dropping Point		None 					ASTM D-2265

Oxidation Stability 		-1					ASTM D-  942

Psi Drop @ 100 hrs

Rust Preventative		1a					ASTM D-1743

No Stain

Water Washout		1.0					ASTM D-1264

Extreme Pressure		45+ (100)					ASTM D-2509

Timken OK Load Kg (Lb)

Four Ball Wear		.6mm					ASTM D-2266

Solids		MoS2

USDA Rating		H-2

Appearance 		Dark Metallic, Tacky

PIN #		                                                             15005

TO ORDER or FOR ADDITIONAL INFORMATION