PRODUCT  DATA  SHEET

G

###### SLC C-4 FLUID

TRANSMISSION

FINAL DRIVE/HYDRAULIC

PRODUCT  DESCRIPTION

Sentinel® SLC C-4 Fluid is a blended synthetic high performance drive train fluid especially formulated for use in transmissions, differential, final drive gear, and hydraulic system requiring a fluid meeting Allison C-4/C-3/C-2 or Caterpillars TO-4/TO-2 requirements.

Sentinel® SLC C-4 Fluid is recommended for the automatic transmission of heavy duty truck and tractor, off highway, construction, earth moving machines and mobile hydraulic systems where operating requirements are severe.

Sentinel® SLC C-4 Fluid is a universal lubricant.  It can be used as the wet brake and power take off fluid and as power steering fluid.

TYPICAL  CHARACTERISTICS

Sentinel® SLC C-4 Fluid has high oxidation resistance and low pour point.  It has extreme pressure additive that provide excellent load carrying capacity and wear protection.  In addition, it is rust and foam inhibited, resists water, and is compatible with commonly used seal materials.  Also, it has a high viscosity index to help insure good high and low temperature performance.

Product Advantages

Long Life Fluid

Non-Corrosive

High Oxidation Stability

Minimize Varnish and Sludge Formation

Excellent Seal Compatibility

Maintains Excellent Low Temperature Flow Properties

Excellent Frictional Control

ISO Viscosity Grade	68					ASTM D-2422

SAE Viscosity Grade	20W

Viscosity cSt @ 100°C 	9.4 					ASTM D-  445

@  40°C	58.3

Viscosity Index     	145					ASTM D-2270

Pour Point ˚C (˚F)	-40 (-40)					ASTM D-    97

Flash Point ˚C (˚F)	225 (437)					ASTM D-    92

Foam Sequence I, II, III	Pass					ASTM D-  892

Demulsibility, 82˚C	40/40/0 (15)					ASTM D- 1401

Rust Test	Pass					ASTM D-665A&B

PIN #						18552

TO ORDER or FOR ADDITIONAL INFORMATION