PRODUCT  DATA  SHEET

G

S-SYNVAC Series

SYNTHETIC

VACUUM PUMP FLUID

PRODUCT  DESCRIPTION

S-SYNVAC Series are super synthetic Vacuum Pump Fluids designed to give excellent service and long fluid life in all types of vacuum pumps. These fluids have very low vapor pressure and very high oxidation resistance. They also have excellent thermal and shear stability

PROPERTIES

S-SYNVAC Series lubricants protect against wear, rust, corrosion and they work on rotary screw, sliding vane, reciprocating and liquid ring vacuum pumps, keeping them free from varnish, carbon, and sludge deposits.

      - Outstanding thermal and oxidation stability and very long fluid life

      - Very high viscosity index for better compressor protection

      - Very low vapor pressure /volatility

      - Excellent coolant properties

      - Extremely high film strength and anti wear properties

      - Very long life fluid allows for extend oil drains

      - Excellent carbon and varnish control to help reduce deposits

      - Excellent rust & corrosion control

TO ORDER or FOR ADDITIONAL INFORMATION

S-SYNVAC Series

SYNTHETIC

VACUUM PUMP FLUID

TYPICAL  CHARACTERISTICS

S-SYNVAC-15                S-SYNVAC-22	     S-SYNVAC-32	               S-SYNVAC-46                               ASTM METHOD

ISO Grade		             15	         22	         32	        46	                  D-2442

Viscosity Index		            129                               125	      123		       130	                                               D-2270

Viscosity cSt @ 40°C		           14.8                               20.1	      33.1	                     47.2		                                 D-445

@100°C		            3.6                                4.3	       5.9		       7.7

Pour Point °F 	               -55                                -53	      -50	                     -45		 	                   D-97

Flash Point °F                                                  386                               398                                   430                                440                                                 D-92

Four Ball Wear, mm 40kg, 1200 rpm      ------------------------------------------------     0.5   ----------------------------------------------

167°F 1Hr,Scar Dia mm                          ------------------------------------------------   0.40   ----------------------------------------------                                        D-2266

Copper Corrosion  24Hr                           -----------------------------------------------     1a     ----------------------------------------------                                        D-130

Rust Test                                                  -----------------------------------------------     Pass   ----------------------------------------------                                       D-665 A+B

Demulsibility, 130°F, 30min                   ----------------------------------------------  40/40/0  ----------------------------------------------                                       D-1401

Vapor Pressure mm Hg @ 80°F               ---------------------------------------------- 0.00005 ----------------------------------------------

Specific Gravity, at 60ºF                            0.817-0.820                  0.821-0.824                    0.825-0.829                   0.830-0.834

Molecular Weight GPC, # AVG                     443                               501                                  554                                  629

Pin #	:                                                             14915                          14922                              14932                              14948

TO ORDER or FOR ADDITIONAL INFORMATION

S-SYNVAC Series

SYNTHETIC

VACUUM PUMP FLUID

TYPICAL  CHARACTERISTICS

S-SYNVAC-68             S-SYNVAC-100	          S-SYNVAC-150	    S-SYNVAC-220                             ASTM METHOD

ISO Grade		    	       68	                  100                            150	           220                               	D-2442

Viscosity Index				  130	                         133                            128		           143			       D-2270

Viscosity cSt @ 40°C		                      68.3                              105                            150		           220			       D-445

@100°C		                      10.0                              13.9                           17.5		            25

Pour Point °F 	                         -43	                  -40			  -40		           -40		 	       D-97

Flash Point °F                                                            460                               514                             525                                530                                               D-92

Four Ball Wear, mm 40kg, 1200 rpm              -------------------------------------------        0.5        --------------------------------------------------                           D-2266

167°F 1Hr,Scar Dia mm                                  -------------------------------------------       0.40       --------------------------------------------------                           D-2266

Copper Corrosion 24Hr                                    -------------------------------------------        1a         --------------------------------------------------                           D-130

Rust Test                                                           -------------------------------------------      Pass       --------------------------------------------------                           D-665 A+B

Demulsibility, 130°F, 30min                           -------------------------------------------    40/40/0     --------------------------------------------------                           D-1401

Vapor Pressure mm Hg @ 80°F                      -------------------------------------------    0.00005     -------------------------------------------------                            D-2266

Specific Gravity, at 68ºF                                   0.834-0.838 (60ºF)           0.839-0.843               0.844 - 0.848                0.849 - 0.853

Molecular Weight GPC, # AVG                               690                                751

Pin #	:                                                                      14968                             14989                         14995                           14998

TO ORDER or FOR ADDITIONAL INFORMATION